Supplementary Information

# Ultrafast Electric Switching of Brookite TiO2 Nanorods with a Permanent Dipole Moment at High Concentrations

Seyed Naveed Hosseini1, Anna G. Nikolaenkova1, Ivan Dozov2, Patrick Davidson2, Patrick J. Baesjou1, Alfons van Blaaderen1, Arnout Imhof1,*

S. N. Hosseini, A. G. Nikolaenkova, P. J. Baesjou, A. van Blaaderen, A. Imhof

Soft Condensed Matter, Debye Institute for Nanomaterials Science, Utrecht University, Princetonplein 1, 3584 CC Utrecht, The Netherlands

E-mail: a.imhof@uu.nl

I. Dozov, P. Davidson

Laboratoire de Physique des Solides, Université Paris-Saclay, CNRS, 91405 Orsay, France

E-mail: patrick.davidson@universite-paris-saclay.fr

Supplementary Figure 1. (a) Transmitted light intensity versus time measured on in-plane switching cells between crossed polarizers containing a brookite TiO2 nanorod dispersion when square d.c. pulses with a pulse width of 5000 μs and a duty cycle of 50% are applied at 3, 7, and 10 V/m field strengths. (b) The same, but zoomed-in around a time when the field is switched off. The dashed vertical lines in red depict the time interval between the two consecutive data points corresponding to the camera’s frame rate of 4000 fps.

Supplementary Figure 2. X-ray diffraction pattern of the titania nanorods compared with the Brookite titania reference (JCPDS No.029-1360). The inset shows an HR TEM image of one nanorod.